LOW MASS MUSCLE ACTUATORS (LoMMAs) USING ELECTRACTIVE POLYMERS

Principal Investigator: Yoseph Bar-Cohen, JPL

Co-Investigators: 	JPL - Tianji Xue, Benjamin Joffe, Shyh-Shiuh Lih and Paul Willis

LaRC - Terry St. Clair, Joycelyn Simpson, Joseph Smith

UNM - Mohsen Shahinpoor

This task develops new miniature actuators that are inexpensive, have low mass, and consume low power to support telerobotic requirements of future NASA missions.  Enabling technologies are being developed using effective electroactive polymers (EAP) to allow miniature mechanisms functions and dexterity for various mission objectives and flight constraints of such programs as Nano-Rover, Mars Explorations and space inflatable structures.  EAPs offer a larger displacement actuation and efforts are being made to develop them to operate like muscles with enhanced force capability.  Also, we are developing mechanisms that employ EAP muscle actuators for effective space telerobotic applications.  The parameters and properties that affect the operation of muscle-actuators in space environment are being investigated.  Issues associated with the servo-control of these actuators will be studied both analytically and experimentally.  Technology products developed in this task include low mass multi-finger gripper, and electrostatically driven muscle actuators that employ tailored electric field.  The scope of the research and development of this task is a laboratory based development for demonstration of the EAP muscle actuators compatibility with Mars environmental conditions.  This task is being carried out by JPL with leading electroactive polymer researchers from the University of New Mexico (UNM) and NASA Langley Research Center (LaRC).

1.	OBJECTIVES

The objective of this task is to develop low-mass, compact, low-cost, and low-power-consuming EAP muscle-actuators for telerobotics and other space applications.  The development of actuators with such characteristics is required for various telerobotic applications including collection and manipulation of surface samples from a rover or directly from a lander.  The emphasis of this task is on the development of effective EAP actuators as well as mechanisms which employ these actuators to demonstrate their applicability to future space programs.  As we are improving our understanding of EAP material behavior and the modeling of the actuation mechanism we are able to produce more effective muscle actuators.  Further, we will investigate the issues of operating the actuators in space environment that include low temperatures and vacuum.  This development of effective EAP muscle actuators is enabling new technologies of end-effectors and manipulators as well as potentially allow controlling the shape and figure of merit of inflatable structures.

Efforts are made in the development of EAP actuators to demonstrate their potential benefit to such NASA applications as micro-manipulators, ultra-dexterous and versatile end-effectors, miniature platforms, inflatable structures, miniature adaptive optics, deployment devices, powered-spacesuit gloves and medical applications.  A servo-controlled multi-DoF EAP-muscle breadboard mechanism will be developed with 30% lower mass, 20% lower volume, and 20% lower power requirements, compared to electroceramic Inchworms.  Inchworms are linear actuators which were space qualified and used on the Telsat series (a series of 6 Hughes satellites which were sponsored by Goddard Space Flight Center in the 70s).

2. 	JUSTIFICATION

Actuators are used to operate telerobotic devices that include robotic arms, rovers, etc.  Other space applications include release mechanisms, antenna and instrument deployment, positioning devices, aperture opening and closing devices, real-time compensation for thermal expansion in space structures, etc.  Increasingly, there are requirements to reduce the size, mass, and power consumption of actuation devices, as well as the cost to NASA.  Electroceramics (piezoelectric and electrostrictive) offer effective, compact, actuation materials to replace electromagnetic motors.  They are used to articulate spacecraft components (e.g. WF/PC II) and to perform various actuation tasks.  A wide variety of Electroactive ceramics (EAC) materials are incorporated into motors, translators and manipulators.  In contrast to electroceramics, EAPs are emerging as new actuation materials with capabilities that cannot be matched by the striction-limited and rigid ceramics [1].  EAP materials are lighter and their potential striction capability can be as high as two orders of magnitude more than EAC materials.  Our efforts are directed to taking advantage of these polymers’ resilience and the ability to engineer their properties to meet NASA articulation requirements.  The mass producability of polymers and the fact that electroactive polymer materials do not require poling (in contrast to piezoelectric materials) help producing them at low cost.  EAP materials can be easily formed in any desired shape and can be used to build MEMS-type mechanisms (actuators and sensors).  They can be designed to emulate the operation of biological muscles [2-5] and they have unique characteristics of low density as well as high toughness, large actuation strain constant and inherent vibration damping.

2.1 	Flight Experiment opportunities and Science Acquisition Benefits

NASA missions planned from 2001 and beyond are considering the use of miniature robotic devices that can potentially employ EAP technology (Mars Exploration and sample collection programs, the New Millennium, Comet Lander and others).  The goal of this LoMMAs Task is to establish alternative actuation-enabling technology for missions that place tight restrictions on mass, size, power, and cost.  Muscle actuators can offer significant advancement in assembly, maintenance, and servicing machines equipped with the functional equivalence of hands.  The EAP muscle actuation capabilities can support scientific experiments that are not possible using large robots.  We are considering the use of muscle actuators to flight experiment applications that include sample acquisition and handling, miniature instrument placement for Mars exploration, and potentially comet landing, shape control of inflatable structures as well as powered spacesuit.

2.2 	Robotic Applications

Muscle actuators that are low mass and consume low power can be considered for various robotic applications including: (a) end effectors with functional characteristics and capabilities similar to those of the human hand; and (b) arms whose capabilities and strength-to-weight ratios are within the range of corresponding biological limbs.

3. 	APPROACH

Our technical approach to reaching the goals of this task, that is requiring interdisciplinary expertise, has been to tackle the issues of developing effective electroactive muscle actuators while seeking effective applications to telerobotic devices of future NASA missions.  Such applications include end-effectors, manipulation devices and inflatable structures.  Because the density of polymers is only about 30% to 50% of the density of electroceramics, EAP muscle actuators are significantly lighter than can be made of EACs or other conventional actuation materials.  Low mass muscle actuators are developed with a large level of displacement and efforts are made to enhance their force actuation capability.  To demonstrate the conformity of the muscles to NASA’s needs the EAP actuators and mechanism will be tested at conditions that are compatible to space environment.  Two categories of EAP actuators are being developed under this task (two related Reports of New technology were submitted): (a) Bending EAP actuators - using perfluorinated ion-exchange membrane metal composites [6], and (b) Linear EAP actuators -  employing tailored-pattern electrodes that allow manipulation of the electric field in electrostatically activated EAPs.

The enhancement of the load carrying capability of the actuator will depend on the success of our efforts to deliver force-actuation and it requires overcoming the limitation of polymers, in terms of stiffness.  The implementation of the most effective EAP materials into muscle actuators is conducted in an iterative manner; as the electroactivity of these materials is enhanced it is incorporated into the design of the muscle-actuator. To allow effective design of the muscle, electro-mechanical analysis is being conducted and the prediction of the performance of the actuator components will be corroborated.  Demonstration devices are developed and they will be subjected to series of electrical, mechanical, and thermal tests to determine the performance envelope of the muscle-actuator, and to form a baseline comparison with conventional EAC mechanisms.  As a goal for the drive capability of a breadboard EAP muscle, it will be designed to have at least 30% lower mass, 20% lower volume, and 20% lower power requirements, compared to an equivalent Inchworm (Burleigh Instruments) linear actuator that is driven by piezoceramics.

FY96 start-up work targeted the development of an electroactive polymer muscle actuator that induces about 10% actuation.  This goal was set in reference to the capability of Shape Memory Alloys (SMA) that induce 8% maximum striction (at a relatively short fatigue life of 1K-cycle).  Compared to EAC, which produce a fraction of a percent actuation, SMAs produce a relatively large displacement and they are increasingly being considered for space applications (e.g., pin-pullers).  Initially, we concentrated our efforts on the use of Polymethylmethacrylates (PMMA) which were reported to produce displacement actuation of more than 10% at certain molecular orientation of its polar elements [7].   However, results of our efforts showed significantly less displacement than the reported level.  Communications via e-mail with the co-authors did not lead to any useful contribution that contradicts our findings.  Our joint efforts with UNM has led to the use of perfluorinated Ion exchange membrane platinum (PIEP) composite films that show a significant bending actuation capability.  A film-pair weighing 0.2-g was configured as a linear actuator and using 5V and 20 mW successfully induced more than 11% contraction displacement.  A single film was used to emulate a miniature bending arm that lifted a mass weighing a fraction of a gram.  Also, the film-pair displayed a significant expansion capability, where a stack of two film-pairs 0.2-cm thick expanded to about 2.5 cm wide (see Figure 1).  Further, a technique of producing complex configuration electrodes was developed to allow forming electrostatically driven polymer films.  A tailored-pattern electroded polymer film was produced (see Figure 2) forming the foundation for muscle elements and a Report of New Technology was submitted.  Moreover, a unique ultrasonic plate wave technique was developed that allows measuring simultaneously the thickness and elastic stiffness constants of thin films.

Figure 1:  PIEP film-pair in expanded mode. A reference pair (top) and an activated pair (bottom).

Figure 2: An electrostatic film with comb-electrodes. The comb connector element is designed to be flexible to contract.

In FY’97, we are developing actuators for sample handling components of a miniature low mass robotic arm that is driven by EAP muscle actuators.  Further, we are enhancing the understanding of the bending actuation mechanism of PIEP composites to obtain 15% stronger force delivering capability.  To demonstrate the performance of muscle-actuators we designed and fabricated a PIEP multi-finger end-effector (See Figure 3 ) in the form of gripper simulating the operation of a hand.  The gripper was mounted on a 5-mm diameter graphite/epoxy arm and was used to lift a 10.3-g rock.  This demonstrator formed a basis for application to sample collection tasks, ultra-dexterous and versatile end-effectors and micro-manipulators.  To enhance the force actuation capability of these EAPs, techniques of producing thicker PIEP films are being developed.  Also, to protect the ionic material constituents of this EAP material, encapsulation methods are being developed. A stronger actuation force is being sought by a better understanding of the actuation mechanism of ionomers as well as searching alternative materials.

Under the linear muscle actuators category, we are continuing to develop the method of manipulating the electric field to allow effective contraction of EAP actuators.  An electric field acting on a film with flat electrodes on both surfaces makes it thinner but wider maintaining a constant volume.  If the film is coated with comb-shaped electrodes placed next to each other on one side, the electroactivated film will shrink laterally.  Once we are successful in our current tests, multilayer actuator will be formed to allow stronger force actuation.  We are currently studying methods of plating interdigital electrodes on thin EAP films and analyzing the effect of the electrodes width, the gap between the electrodes and the thickness of the film.  Further, we are considering the use of a dual-sided film with various combinations of polarization to control the direction of the electric field.

Figure 3: An end-effector gripper lifting 10.3-g rock under 5-V, 25-mW activation using four 0.1-g fingers made of perfluorinated ion-exchange membrane platinum composite.

In FY’98, we will continue the development of the two categories of EAP muscle-actuators with emphasis on applications to telerobotics.  In order to optimize the design and performance of the actuators, analytical modeling will be made that incorporates the characteristics of EAPs and the parameters that affect their performance. We will continue seeking EAP materials and electroactivation methods of enhancing the actuation force of the muscle actuators.  Further, we will demonstrate the operation of muscle actuators in a robotic mechanism with high dexterity, low mass and low power consumption.

The ionomer muscle actuator will be characterized to determine design parameters for the robotic demonstrator. We are going to model the conduction processes of the composite ionomer using impedance spectroscopy.  AC conductivity data as a function of frequency will be acquired and analyzed.  Also, stress-strain analysis will be conducted and an electro-mechanical simulation will be developed. The validity of this simulation model will be corroborated experimentally. The developed model will be used to produce enhanced ionomer composite actuators with better performance.  During the modeling process alternative ionomer composite systems will be explored to obtain a stronger force actuation capability.

The dual-side tailored-pattern electroded EAP actuator will be developed.  This electroding structure allows a flexible manipulation of the electric field to generate electrostatic forces on the film to control the dimensions and shape of the EAP actuator. A simplified illustration is shown in a cross-section view (see Figure 4), where a patterned electrodes are plated symmetrically on the two sides. The actuation is based on the electrostatic principle that a pair of adjacent electrodes repel or attract each other depending on their polarity.  An operational model for the tailor field would need to be established to take both the electrostrictive forces and the electrostatic (i.e. coulomb)  force into account.  The understanding of the role of the various physical and material parameters is important for the enhancement of the capability of the actuator. As stated earlier, once the film concept is demonstrated, efforts will be made to develop the fiber muscle elements as shown in Figure 5.  The fiber will be coated helically with two electrodes running parallel along the fiber, where one electrode ending further away than the other at each end of the fiber.  Thus, each end of the fiber will serve as a pole of the EAP activation electrodes.  Tests will take place to optimize the design of the fiber elements and the muscle will be formed later as a bundle of helically-electroded EAP fibers.  The fiber redundancy in the bundle will provide a high reliability to the muscle as well as a stronger force.

Figure 4:  Tailored pattern electrodes are inducing an electrostatic field to cause extension and contraction, respectively.

Figure 5:  Helical electrodes and an EAP fiber forming an element of a muscle.

The developed muscle actuators will be incorporated into a robotic arm and end-effector that will perform manipulation and sample collection task. The performance of the robotic arm will be enhanced by the combined use of the (a) PIEP actuator as the end-effector and (b) the tailored pattern electrostatic actuator as the lifter.  Where the mass holding capability will be increased by 20% and the arm lifting capability by 15% over FY’97.   Tests will be conducted with this robotic setup that is fully actuated by EAP muscles and the performance will be recorded to form a base-line comparison with existing EAC actuation mechanisms.

In FY’99, we plan to develop servo-control techniques for the precision drive of miniature mechanism that are operated by EAP muscle actuators.  Further, we intend to complete the development of a testbed for the characterization of EAP muscle actuators at low temperatures and vacuum conditions to simulate Mars environment.  The issue of operating EAP actuators at Mars environment will be addressed and test will be made to demonstrate the ability to operate at such conditions.

In FY’00, we will bring the development of the EAP muscle actuators closer to operability to flight related applications.  While continuing the research and development of the EAP muscle actuators technology for telerobotic applications, we intend to demonstrate the operation of EAP muscles in multi-DoF dexterous robotic system.  The multi-DoF system that will be driven by EAP muscle actuators which will be integrated into a sample manipulation testbed.  Tests will be made using the EAP robotic system to perform tasks that are dictated by the requirements of a  potential mission.

3.1      LEVEL 1 DEMONSTRATION MILESTONES

The following describes the LoMMAs Task Level 1 milestones for this task.  A test sequence of gradually increasing complexity in the terrestrial atmosphere are driving this task.

- Modeling perfluorinated ion-exchange membrane platinum composite EAP	Q2 FY98

- Develop a testbed for performance evaluation at Mars environment	Q3 FY98

- Modeling and development of multi-element muscle actuator	Q4 FY98

- Demonstrate muscle action in a robotic operation	Q4 FY98

- Servo-control and miniature EAP drive electronics	Q3 FY99

- Low temperature operation testing of EAP muscle actuators	Q4 FY99

- Demonstrate multi-DoF dexterous robotic arm 	Q2 FY00

- EAP-driven multi-DoF arm integration into a sample manipulation testbed	Q4 FY00

4. 	PARTICIPANTS

This task is a conducted in cooperation with Dr. Mohsen Shahinpoor, Director, Intelligent Materials, Structures & Systems Lab, University of New Mexico (UNM), as well as, Dr. Joycelyn Simpson and Dr. Joseph Smith of LaRC, under the supervision of Dr. Terry St. Clair, Manager, Composites and Polymers Branch.  This cooperation with UNM is done under a subcontract that is funded by this task and with LaRC under a direct NASA HQ fund transfer from this task.  Further, LoMMAs was selected as one of the graduate students projects (5 students for 9 month) by the Integrated Manufacturing Engineering of UCLA (no cost to the task).  In addition, we are working in collaboration with the SRI International team who has been involved with electrostatically driven polymers R&D for more than four years.  Potential companies that are considered for the commercialization of the technology include QMI (Costa Mesa, CA) with whom the JPL Principal Investigator currently has a Technology Cooperative Agreement in the area of ultrasonic motors (under the Planetary Dexterous Manipulator Task, which is also funded by Code S).

5. 	DELIVERABLES

The proposed program is establishing a enabling technology of actuators that supports the NASA goals of cheaper, smaller, and better.  It will enable the production of new types of telerobots for future NASA missions.  An EAP-muscle breadboard will be demonstrated to have a 30% lower mass, 20% lower volume, and 20% lower power requirements, compared to an equivalent Inchworm (Burleigh Instruments) that is driven by piezoceramics.  While it may be premature to state actual cost estimates for the muscle-actuator, it is anticipated that these types of devices will be significantly cheaper to fabricate than any equivalent electroceramic device.  To demonstrate the applicability of EAP-muscles to space application, an multi-DoF manipulator that is driven simulating a hand will be produced and the performance envelope will be determined at simulated Mars environment.

6. 	COMMERCIALIZATION POTENTIAL

The low cost and mass production potential of EAPs opens a wide range of commercial applications, including actuation of mechanisms in automobiles and consumer products.  Artificial muscles for medical applications are another important application of EAP actuators.  Most biological joints are controlled by an antagonistic system of contracting muscles, much the same way as our own biceps-triceps antagonistic muscle system articulates our arms.  A linear contracting actuators, built as a result of this effort, can be used to manipulate skeletal (e.g., human) systems.  The UNM research team has already experimented with this concept designing attire, boots, and gloves that can be worn externally and actuate an internal structure such as an astronaut's hands, legs, and feet in space or on other planets.   Dr. Robert Siegel, Director, Cardiac Noninvasive Laboratory, Cedars-Sinai Medical Center, has expressed a strong interest in implementing the results of this LoMMAs Task.

7. 	FUNDING REQUIREMENTS

|  | FY96 | FY97 | FY98 | FY99 | FY00 |
| --- | --- | --- | --- | --- | --- |
| NASA Funding Profile ($K): | 200 | 200 | 250 | 220 | 220 |
| Full Time Equivalents (WY): | .5 | .5 | .7 | .6 | .6 |

8.  FACILITIES

JPL has established the capability to produce some of the EAP materials and muscle actuators as well as characterize their performance.  The NDE and Advanced Actuators lab has the required instrumentation to determine the displacement performance of muscle actuators under controlled conditions as well as measure their electromechanical response.  A large number of electrical parameters can be analyzed using a Schlumberger Impedance Analyzer, Model 1260.  For the temperature control at vacuum conditions, a custom-modified Janis ST-400 system will be used.  This system allows tests at high vacuum up to 10-6 torr, at the temperature range of 77K to 450K.  Actuation electronics, data acquisition, and processing hardware/software are also available.  To determine the performance of actuators in vacuum conditions under thermal and mechanical loads, the Lab’s SATEC custom-designed system will be used.  This lab has also the capability to perform non destructive evaluation to determine the integrity of the muscle actuators and structures.

NASA LaRC has significant expertise in the synthesis of high performance electroactive polymers.  LaRC is the facility that is producing the required polymer films and fibers in different sizes and shapes to accommodate the required actuator designs.  The active elements are processed at the Smart Materials Laboratory which has the capability of electroding and electrically poling polymer films and fibers to produce both piezoelectric and electrostrictive polymers.  The Smart Materials Laboratory also has the capability to evaluate the polymers polarization potential and ferroelectric hysteresis behavior.

The Artificial Muscles Research Institute at the University of New Mexico is equipped with an array of robotic manipulators, artificial muscles material characterization equipment such as computer-controlled ovens, ultrasonic baths, computer-controlled chemical processing equipment, assortment of measuring instruments,  a 5-watt Argon laser system, computer-controlled furnaces and ventilation hoods, refrigerators and freezers, microscopes, a large chemical inventory, computer-controlled data acquisition systems, computer-controlled signal generators, measuring devices and multimeters, and a two experimental setups to characterize and test active materials as well as mechanisms in the form of artificial muscles. The Institute also has access to a physical vapor deposition system, SEM as well as rapid prototyping laboratories at UNM School of Engineering.

9. 	PRINCIPAL INVESTIGATORS

Dr. Yoseph Bar-Cohen is the Task Manager of the LoMMAs program (two new Reports of New Technology).  He is a member of the Technical Staff responsible for the advanced actuation technologies in the Science and Technology Development Section at JPL.  Since joining JPL in 1991, he has established state-of-the-art Advanced Actuation and NDE Labs.  He received his Ph. D. in Physics from the Hebrew University at Jerusalem, Israel, in 1979.  He has more than 26 years experience in areas related to sensors, actuation materials, and NDE, including positions at the Israel Aircraft Industry, SRL at the Air Force Materials Laboratory and McDonnell Douglas Corporation.  He is currently developing ultrasonic motors for the Planetary Dexterous Manipulator task (filed 1 patent and 3 pending) and developed a crawler that can walk on structures using suction cups and ultrasonic motor actuators .  He is the author of more than 120 publications and holds many patents.  He is an Adjunct Professor at the University of California, Los Angeles (UCLA) and a Fellow of the American Society for Nondestructive Testing.

Dr. Tianji Xue joined the JPL’s NDE&AA team in June, 1996. He obtained his Ph.D. and M.S. degrees in Electrical Engineering from Iowa State University and B.S. degree in Optical Engineering from the Beijing Institute of Technology. He is experienced in solid state materials and devices, thin film technology, optical system design and image processing, digital signal processing, and statistical data analysis. He has been also active in the numerical modeling of electromagnetic and ultrasonic wave propagation with application to NDE. At JPL, he is responsible for the design, testing and simulation of telerobotic actuators based on EAP. He is also involved in software design for automatic measurement instrument control, data acquisition and analysis.

Dr. Benjamin Joffe is a mechanical engineer with over 36 years of experience in the areas of electromagnetic system design and the development of precision mechanisms.  He has worked at JPL since 1991, and is Cognizant Engineer for the Cassini Engine Gimbal Actuators.  Prior to coming to JPL, he worked for  American Semiconductor Equipment Technologies, where he designed high-speed, sub-micron, precision machinery for semiconductor fabrication.  From 1967 to 1978, he was Senior Scientist and head of the Magnetic Equipment Department at the Academy of Sciences Institute of Physics, in Riga, Latvia.  He performed extensive research on the interaction of electromagnetic and electrical fields for the purpose of manipulating and orienting parts for assembly line applications.  He holds a Master’s Degree in Mechanical Engineering from the Riga Polytechnic Institute, and a Ph. D. in Machine Design from the Latvian Academy of Sciences.  Dr. Joffe is the author of over 50 scientific and technical publications, 25 U.S. Patents and over 200 patents in other countries.  He has received many awards for innovation in mechanisms and other unique inventions.

Dr. Shyh-Shiuh Lih is a Member of Technical Staff of  the Advanced Materials and Fluid Processes Technology Group, Science and Technology Development Section (354).  Since joining JPL in February 1995, he has been active in R&D of ultrasonic motors, electro-elastic actuators and nondestructive evaluation (NDE) techniques for space applications. His technical expertise also includes the areas of dynamic response of composite structures, mechanics of advanced materials and structures.  He has been a consultant to JPL since 1993 when he developed and performed a series of ultrasonic experiments to characterize the elastic properties of composite materials, adhesive joints, and damping of materials. He also developed an innovative technique for the prediction of the localized elastodynamic response of composite laminates subject to transient surface loadings, when he was a research engineer at UCLA from 1992-1994.  He received his Ph.D. (Mechanical/Engineering) from UCLA, in 1992.

Dr. Mohsen Shahinpoor is a robotics and intelligent systems design professor and director of Artificial Muscles Research Institute as well as Intelligent Materials, Structures and Systems Laboratory at the University of New Mexico.  He holds several patents on robotic electromechanical actuators and artificial muscle systems (see U.S. Patent 5,250, 167).  His shape-memory alloy actuator system is currently used by Sandia National Laboratories scientists for intelligent dynamic shape control of large mirrors.  He has also been involved, as a research team member, in the design and fabrication of a micro-miniaturized robotic linear actuator system (the world's smallest robot) with research scientists at Edwards Air Force Base, (Dr. Wesley Hoffman) as well as at Hughes-STX (Martin Buemeister).  He is a registered, licensed professional engineer and holds a Ph.D. in Mechanical and Aerospace Engineering. He is the discoverer of a two new effects in ionic polymeric gels and platinum ion exchange polymer (PIEP) composites.

Dr. Joycelyn Simpson is a chemical engineer in the Composites and Polymers Branch of the Materials Division at LaRC.  She has established a Smart Materials Laboratory for developing high performance electroactive polymers for aerospace applications.  Dr. Simpson has expertise in dielectric analysis of polymeric systems.  Moreover, she has experience in processing polymeric and composite materials to induce an electroactive response.  She received B.S. degrees in chemistry and in chemical engineering from Spelman College and the Georgia Institute of Technology.  Subsequently, she earned M.S. and Ph.D. degrees in chemical engineering from the Georgia Institute of Technology in 1989 and 1993, respectively.

Dr. Joseph G. Smith Jr. is a Polymer Scientist, Composites and Polymers Branch, Materials Division, at LaRC.  He is responsible for fundamental and applied research and development on high performance structural resins for the aerospace industry.  He received his B.S. degree from High Point College, 1985, and Ph. D. degree from Virginia Commonwealth University, 1990.  Prior to his affiliation with LaRC, he held faculty research positions at the University of Akron and Virginia Commonwealth University.  He has 14 Refereed Journal Publications (includes 2 Book Chapters), 21 Other Referenceable Publications, 10 Technical Presentations, 5  Patents and 5 NASA Tech Briefs.  In 1994, Dr. Smith was the Co-Inventor of the Year at LaRC.

Dr. Terry St. Clair is the head of the Composites and Polymers Branch of the Materials Division at LaRC.  He received a B.S. in chemistry from Roanoke College and a Ph.D. in organic Chemistry from Virginia Tech.  Dr. St. Clair is a noted expert in the synthesis and characterization of high performance polymers.  He has authored in excess of fifty papers and thirty patents on polyimides and other high performance polymers used in the aerospace, adhesive, and electronics industries.

Paul B. Willis is a polymer chemist in the Mechanical Engineering Section of JPL.  After graduate work in the Polymer Science Department of the University of Massachusetts, he worked in industry doing contract research and development for ten years, prior to joining JPL in 1988.  His primary areas of interest include polymer synthesis, surface chemistry, composites, adhesives, life analysis, and applied mechanics.  He has more than twenty years experience in commercial and aerospace technologies.  He currently holds the position of Senior Research Engineer.

10.	REFERENCES

- Furukawa and J. X. Wen, “Electrostriction and Piezoelectricity in Ferroelectric Polymers,” Japanese Journal of Applied Physics, Vol. 23, No. 9, (1984), pp. 677-679.

- Ian W. Hunter and Serge Lafontaine, “A comparison of muscle with artificial actuators,” IEEE Solid-State Sensor and Actuator Workshop, 1992, pp. 178-165.

- M. Shahinpoor, "Continuum electromechanics of ionic polymeric gels as artificial muscles for robotic applications," Smart Materials and Structures, V 3, pp. 367-372, 1994.

- Roy Kornbluh, Ron Pelrine and Jose Joseph, “ Elastomeric dielectric artificial muscle actuators for small robots,” Proceeding of the 3rd IASTED International Conference, June, 14-16, 1995.

- Ron Pelrine, Roy Kornbluh, Jose Joseph and Seiki Chiba, “Artificial muscle actuator,” Proc. of the First International Micromachine Sym., Nov. 1-2, 1995, pp 143-146.

- “Recent advances in perfluorinated ionomer membranes: Structure, properties and applications,” Journal of Membrane Science, V 120, No. 1, Oct. 1996, pp 1-33.

- Ohara, K., et al, “Electrostriction of Polymethylmethacrylates”, Colloid and Polymer Science, Vol. 260 (1982), pp. 164-168.

REPORTS OF NEW TECHNOLOGY AND PUBLICATIONS

- Y. Bar-Cohen, B. Joffe and J. Simpson, “Electroactive Muscle Actuators (EMA),” New Technology Report, Item No. 9649, Docket 20017, August 22, 1996.

- Y. Bar-Cohen, T. Xue, M. Shahinpoor (UNM) and S.-S. Lih., "Multi-Finger Electroactive Polymer Gripper (MEPG)" , Submitted as a Report of New Technology, January 17, 1997.

- Y. Bar-Cohen, T. Xue, B. Joffe, S.-S. Lih, P. Willis, J. Simpson, J. Smith, T. St. Clair, M. Shahinpoor, “Low Mass Muscle Actuators (LoMMAs) Using EAP,” Smart Structures and Materials Symposium, Enabling Technologies: Smart Structures and Integrated Systems, San Diego, CA, 3-6 March 1997.

POINT OF CONTACT

Yoseph Bar-Cohen, Ph. D. (PI),

yosi@jpl.nasa.gov,

(818) 354-2610 (Voice), (818) 393-4057 (Fax)